| Qualification Results Summary of ADXL362, ADXL363 Sensor Wafers on 8" MEMS Only Process at TSMC fab3 |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Early Life Fail (ELF) | MIL-STD-883 M1015 | 3x800 | PASS |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3x77 | PASS |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3x77 | PASS |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3x77 | PASS |
| Unbiased Highly Accelerated Stress Test (UHAST) * | JEDEC JESD22-A118 | 3x77 | PASS |
| Low Temperature Storage (LTS) | JEDEC JESD22-A119 | 3x77 | PASS |
| Low Temperature Operating Life (LTOL) | JEDEC JESD22-A108 | 3x77 | PASS |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3x77 | PASS |
| Mechanical Shock Powered | IEC 68 Part 2-27 Testgroup Ea | 4x10 | PASS |
| 1.2m Random Drop | CAM0091 | 7x35 | PASS |
| 1.2m Guided Drop | IEC 60068-2-32 | 5x5 | PASS |
| Group D Sub Group 4 | MIL-STD-883 M5005 | 3x15 | PASS |
| FICDM | JESD22-C101 | 1x3 | PASS |
| HBM | ESDA/JEDEC JS-001-2011 | 1x3 | PASS |
| MM | JESD22-A115 | 1x3 | PASS |
| LU | JEDEC-JESD78 | 1x6 | PASS |

*Preconditioned per JEDEC/IPC J-STD-020