Analog Devices Inc, Hillview Assembly Site Transfer

Qualification Results and Summary of Golden Altos Assembly of

TO39 for RH and SMD devices

| Test | Specification to MIL-STD-883 | Sample Size total of 2 lots | Results |
| --- | --- | --- | --- |
| B/2a | Resistance to Solvents Method 2015 | 3 units | PASS |
| B/2b | Internal Visual and Mechanical Method 2013/2014 | 4 units | PASS |
| B/2c | Bond Pull Method 2011 | 44 bonds | PASS |
| B/2d | Die Shear Method 2019 | 6 units | PASS |
| B/3 | Solderability Method 2003 | 48 leads | PASS |
| B/5 | Pre-test 3 temp. | 160 units | PASS |
|  | Steady-State Life Method 1005 Cond. C 150C/ 500hrs | 160 units | PASS |
|  | Post-test 3 temp. | 160 units | PASS |
| B/6 | Pre-test 3 temp. | 34 units | PASS |
|  | Temp. Cycling Method 1010, Cond. C | 34 units | PASS |
|  | Constant Acceleration Method 2001, Cond. E | 34 units | PASS |
|  | Fine Leak/Gross Leak Method 1014, Cond. A and C | 34 units | PASS |
|  | Post-test 3 temp. | 34 units | PASS |
| D/1 | Physical Dimensions Method 2016 | 30 units | PASS |
| D/2 | Lead Integrity Method 2004, Cond. B2 | 90 leads | PASS |
|  | Fine Leak/Gross Leak Method 1014, Cond. A and C | 90 leads | PASS |
| D/3 D/3 | Pre-test 3 temp. | 34 units | PASS |
|  | Thermal Shock Method 1011, Cond. B | 34 units | PASS |
|  | Temperature Cycling Method 1010, Cond. C | 34 units | PASS |
|  | Moisture Resistance Method 1004 | 34 units | PASS |
|  | Fine Leak/Gross Leak Method 1014, Cond. A and C | 34 units | PASS |
|  | Visual Examination Method 1004/1010 | 34 units | PASS |
|  | Post-test 3 temp. | 34 units | PASS |
| D/4 | Pre-test 3 temp. | 34 units | PASS |
|  | Mechanical Shock Method 2002, Cond. B | 34 units | PASS |
|  | Vibration Variable Frequency Method 2007, Cond. A | 34 units | PASS |
|  | Constant Acceleration Method 2001, Cond. E | 34 units | PASS |
|  | Fine Leak/Gross Leak Method 1014, Cond. A and C | 34 units | PASS |
|  | Visual Examination Method 1010/1011 | 34 units | PASS |
|  | Post-test 3 temp. | 34 units | PASS |
| D/5 | Salt Atmosphere Method 1009, Cond. A | 30 units | PASS |
|  | Fine Leak/Gross Leak Method 1014, Cond. A and C | 30 units | PASS |
|  | Visual Examination Method 1009 | 30 units | PASS |
| D/6 | Internal Water Vapor Method 1018 | 6 units | PASS |
| D/7 | Adhesion of Lead Finish Method 2025 | 30 leads | PASS |