a

PCN 09_0101 – Summary of Available Qualification Data

| Test | Conditions | Sample Size | Results |
| --- | --- | --- | --- |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 462 | Pass |
| Temperature Cycle* | JEDEC JESD22-A104 | 1155 | Pass |
| Solder Heat Resistance (SHR) | ADI-0049 | 33 | In progress Expected completion 6/15/2009 |
| Autoclave* | JEDEC JESD22-A102 | 770 | Pass |
| High Temperature Storage | JEDEC JESD22-A103 | 231 | Pass |
| Latch-Up | JEDEC Standard 78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESD Association STM5.1-2001 | 24 | 3500V |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | 15 | 1500V |

*Preconditioned Per JEDEC/IPC J-STD-020