QFP Transfer Qualification Results

| Package | Assembly Site | Autoclave | Solder Heat Resistance | Temp Cycle | HTS |
| --- | --- | --- | --- | --- | --- |
| 52 Lead 10x10 MQFP | SCC | Pass | Pass | Pass | Pass |
| 80Lead 14x14 LQFP | SCC | Pass | Pass | Pass | Pass |
| 48Lead 7x7 LQFP | SCC | Pass | Pass | Pass | Pass |
|  |  | 0/441 | 0/99 | 0/441 | 0/441 |