| PCN # 09_0260 Reliability Report – RQR8071 |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL) | JEDEC JESD22-A108 | No. of lots = 1 Sample Size/lot = 45 | Pass |
| Unbiased Highly Accelerated Stress Test (UBHAST) | JEDEC JESD22-A118 | No. of lots = 3 Sample Size/lot = 45 | Pass |
| Temperature Cycle (TC) | JEDEC JESD22-A104 | No. of lots = 3 Sample Size/lot = 45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | No. of lots = 1 Sample Size/lot = 45 | Pass |
| Latch up | JESD-78 | No. of lots = 1 Sample Size/lot = 6 | Pass |
| Electrostatic Discharge Human Body Model | ESD Assoc. STM5.1-2001 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |
| Electrostatic Discharge Machine Model | ESD Assoc. STM5.2-1999 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |