| PCN # 09_0260 Reliability Report – RQR8472 |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Electrostatic Discharge Human Body Model | ESD Assoc. STM5.1-2001 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |
| Electrostatic Discharge Machine Model | ESD Assoc. STM5.2-1999 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | No. of lots = 1 Sample Size = 3 samples/voltage | Pass |