| PCN09_0276 QUAL TESTS |  |  |  |
| --- | --- | --- | --- |
| PREVIOUS QUALIFICATION TESTS COMPLETED 2-aug-2004 VIA pcn04_0054 |  |  |  |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 Tj = +150C | 3 lots, 45 (0) ea | Pass |
| Early Life | 48 hrs Ta = +125C | 3 lots, 667(0) ea | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3 lots, 45 (0) ea | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 500 cycles, -65/+150C | 3 lots, 45 (0) ea | Pass |
| Thermal Shock | 500 cycles, -65/+150C | 45(0) | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 121C, 100% RH, 2atm | 3 lots, 45(0) ea | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 1000 hrs @ +150C | 1 lot, 45(0) ea | Pass |
| Latch-Up | JEDEC Standard 78 Class I Level A | 6 | Pass, no latchup occurred |
| Electrostatic Discharge Human Body Model | ESD Association STM5.1-1998 | 24 | Pass 500V Class 1B |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | 15 | Pass 250V Class C3 |
| Electrostatic Discharge Machine Model | ESD Association STM5.2-1999 | 12 | Pass 200V Class M3 |

| PCN09_0276 |  |  |  |
| --- | --- | --- | --- |
| QUALIFICATION TESTS TO BE PERFORMED ON Class S QMLR GRADE ONLY |  |  |  |
| Test | Conditions | Sample Size | Est. Compl. Date |
| Group A | All Table I Parameters per 5962-85127 +25, -55 & +125C | 116 (0) | May, 2010 |
| Group B: Resistance to Solvents Bond Strength Die Shear Solderability | TM2015 TM2011 TM2019 TM1003 | 3(0) 4(0) wires 3(0) 3(0) | May, 2010 |
| Group C | 1000 Hrs @ +125C Ta Mil-Std-883 TM1005 | 45(0) | May, 2010 |
| Group D: Subgroup 1: Physical Dims Subgroup 2: Lead Integrity Hermeticity Subgroup 3: Thermal Shock Temp Cycle Moisture Resistance Hermeticity Visual Exam End-Point Electrical Subgroup 4: Mechanical Shock Var. Freq. Vibration Constant Acceleration Hermeticity Visual Exam End-Point Electrical Subgroup 5: Salt Atmosphere Hermeticity Visual Exam Subgroup 6: Internal Water Vapor Subgroup 7: Adhesion of Lead Finish Subgroup 8: Lid Torque | TM2016 TM2004 TM1014 TM1011 TM1010 TM1004 TM1014 TM1004 5962-85127 TM2002 TM2007 TM2001 TM1014 TM2009 5962-85127 TM1009 TM1014 TM1009 TM1018 TM2025 TM2024 | 15(0) 15(0) “ 15(0) “ “ “ “ “ 15(0) “ “ “ “ “ 15(0) “ “ 3(0) 3(0) 5(0) | May, 2010 |
| Group E | Mil-Std-883, TM1019 Total Ionizing Dose Dose Rate 50-300 rad(Si)/sec | 2(0) die per wafer | Complete, Pass |
| Radiation (Low Dose Rate) | Total Ionizing Dose Dose Rate  10 mrad(Si)/sec | 2(0) die per wafer | *Contact Factory for Test Results |