| Package | Assembly Site | Autoclave1 121°C, 100%RH, 2 atm, 96 hrs | HAST1 130C 85%RH 2atm, Biased | HTS 150°C, 1000 hrs | Temp Cycle1 -65°C to 150°C, 500 cycles |
| --- | --- | --- | --- | --- | --- |
| TSOT | Carsem | Pass | Pass | Pass | Pass |
|  | TOTAL: | 0 fails/641 samples | 0 fails/82 samples | 0 fails/209 samples | 0 fails/641 samples |

QUALIFICATION RESULTS: PCN 10_0007

1 Parts subjected to preconditioning per J-STD-0020, MSL 1 with peak reflow temperature of 260°C prior to stress