Report Title:	AD9122 Die Revision (Rev. A)

Report Number:	8508

Revision:	A

Date:	10 March 2010

Summary

This report documents the successful completion of the reliability qualification requirements for release of the AD9122 die revision. AD9122 is a dual, 16-bit, 1200MSPS, TxDAC digital-to-analog converter, in a 72-LFCSP package.

Table 1: AD9122 Product Characteristics

| Die/Fab |  |
| --- | --- |
| Die ID | AD9122 |
| Die Size (mm) | 4.73 x 4.68 |
| Wafer Fabrication Site | TSMC Fab-8B |
| Wafer Fabrication Process | 0.18µm CMOS |
| Transistor Count | 2 million |
| Passivation Layer | undoped-oxide/SiN |
| Bond Pad Metal Composition | AlCu |

| Package/Assembly |  |
| --- | --- |
| Available Package | 72-LFCSP |
| Body Size (mm) | 10.00 x 10.00 x 0.85 |
| Assembly Location | Amkor-K |
| Molding Compound | Sumitomo G700 |
| Wire Type | Gold MKE-UB |
| Wire Diameter (mils) | 1.00 |
| Die Attach | Ablestik 8290 |
| Lead Frame Material | Copper |
| Lead Finish | Tin Plate |
| Moisture Sensitivity Level | 3 |
| Maximum Peak Reflow Temperature (°C) | 260 |

Description / Results of Tests Performed

Tables 2 and 3 provide a description of the qualification tests conducted and the associated test results for products manufactured on the same technologies as described in Table 1. All devices were electrically tested before and after each stress. Any device that did not meet all electrical data sheet limits following stressing would be considered a valid (stress-attributable) failure unless there was conclusive evidence to indicate otherwise.

Table 2: LFCSP at Amkor-K Package Qualification Test Results

| Test Name | Spec | Conditions | Device | Lot # | Sample Size | Qty. Failures |
| --- | --- | --- | --- | --- | --- | --- |
| Autoclave (AC)1 | JESD22-A102 | 121°C 100%RH 2atm 168 hours | AD9389A | Q5731.1 | 45 | 0 |
|  |  |  |  | Q5731.5 | 45 | 0 |
|  |  |  |  | Q5731.9 | 45 | 0 |
|  |  | 121°C 100%RH 2atm 96 hours | AD53565 | Q6670.1 | 45 | 0 |
|  |  |  |  | Q6670.2 | 45 | 0 |
|  |  |  |  | Q6670.3 | 45 | 0 |
|  |  |  | AD8158 | Q6741.2 | 32 | 0 |
|  |  |  |  | Q6741.3 | 32 | 0 |
|  |  |  |  | Q6741.4 | 32 | 0 |
| Biased HAST (HAST)1 | JESD22-A110 | 130°C 85%RH 2atm, Biased 96 hours | ADUC824 | F154193.4 | 44 | 0 |
|  |  |  |  | F154212.4 | 45 | 0 |
|  |  |  | AD9389A | Q5731.10 | 45 | 0 |
|  |  |  |  | Q5731.2 | 45 | 0 |
|  |  |  |  | Q5731.6 | 45 | 0 |
| High Temperature Storage Life (HTSL) | JESD22-A103 | 150°C 1,000 hours | AD53565 | Q6670.9 | 45 | 0 |
|  |  |  | AD8158 | Q6741.1 | 32 | 0 |
|  |  |  | X148 | Q4236.2 | 45 | 0 |
| Solder Heat Resistance (SHR)1 | ADI-0049 | See Footer | AD9122 | Q8508.5 | 30 | 0 |
| Temperature Cycling (TC)1 | JESD22-A104 | -65°C / +150°C 1,000 cycles | AD9863 | Q3716.9 | 45 | 0 |
|  |  | -65°C / +150°C 500 cycles | AD9849 | Q3716.5 | 45 | 0 |
|  |  | -55°C / +125°C 1,000 cycles | AD53565 | Q6670.14 | 45 | 0 |
|  |  |  |  | Q6670.15 | 45 | 0 |
|  |  |  |  | Q6670.16 | 45 | 0 |
| Temperature Humidity Bias (THB)1 | JESD22-A101 | 85°C 85%RH, Biased 1,000 hours | AD53565 | Q6670.17 | 45 | 0 |
|  |  |  |  | Q6670.18 | 42 | 0 |
|  |  |  |  | Q6670.19 | 45 | 0 |
|  |  |  |  | Q6670.25 | 45 | 0 |

- These Samples were subjected to preconditioning (per J-STD-020 Level 3) prior to the start of the stress test. Level 3 preconditioning consists of the following:

- Bake: 24 hrs @ 125ºC,

- Soak: Unbiased Soak: 192 hrs @ 30ºC, 60%RH,

- Reflow: 3 passes through an oven with a peak temperature of 260ºC.

Table 3: 0.18µm CMOS at TSMC-8B Process Qualification Results

| Test Name | Spec |  | Conditions | Device | Lot # | Sample Size | Qty. Failures |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Early Life Failure Rate (ELFR) |  | MIL-STD-883, Method 1015 | 125°C 48 hours | ADAU1401 | Q5834.21 | 200 | 0 |
|  |  |  |  |  | Q5834.22 | 200 | 0 |
|  |  |  |  |  | Q5834.20 | 200 | 0 |
|  |  |  |  |  | Q5834.23 | 200 | 0 |
|  |  |  |  |  | Q5834.26 | 200 | 0 |
|  |  |  |  |  | Q5834.25 | 200 | 0 |
|  |  |  | 150°C 48 hours | ADW15000 | Q6115.37 | 245 | 0 |
|  |  |  |  |  | Q6115.38 | 243 | 0 |
|  |  |  |  |  | Q6115.39 | 245 | 0 |
| Biased HAST (HAST) |  | JESD22-A110 | 130°C 85%RH 2atm, Biased 96 hours | AD9930 | Q5552.1 | 32 | 0 |
| Biased HAST (HAST)1 |  | JESD22-A110 | 110°C 85%RH 2atm, PWR CYC 96 hours | ADW15000 | Q6115.8 | 77 | 0 |
|  |  |  |  |  | Q6115.15 | 77 | 0 |
|  |  |  |  |  | Q6115.21 | 77 | 0 |
|  |  |  | 130°C 85%RH 2atm, Biased 96 hours | AD9352 | Q6289.1 | 45 | 0 |
|  |  |  |  | AD9779 | Q5325.8 | 32 | 0 |
|  |  |  |  | ADAU1401 | Q5834.17 | 45 | 0 |
|  |  |  |  |  | Q5834.15 | 45 | 0 |
| High Temperature Operating Life (HTOL) |  | JESD22-A108 | 125°C ‹ Tj ‹ 135°C, Biased 1,000 hours | ADW15000 | Q6115.11 | 77 | 0 |
|  |  |  |  |  | Q6115.18 | 77 | 0 |
|  |  |  |  |  | Q6115.12 | 77 | 0 |
|  |  |  | 135°C ‹ Tj ‹ 150°C, Biased 750 hours | AD80150 | Q6342.17 | 45 | 0 |
|  |  |  |  | AD9352 | Q6289.2 | 45 | 0 |
|  |  |  | 150°C ‹ Tj ‹ 175°C, Biased 500 hours | AD9779 | Q5325.9 | 32 | 0 |
|  |  |  |  | ADAU1401 | Q5834.18 | 45 | 0 |
|  |  |  |  |  | Q5834.16 | 45 | 0 |
| High Temperature Storage Life (HTSL) |  | JESD22-A103 | 150°C 1,000 hours | AD80150 | Q6342.16 | 45 | 0 |
|  |  |  |  | AD9930 | Q5552.2 | 32 | 0 |
|  |  |  |  | ADAU1401 | Q5834.14 | 45 | 0 |
|  |  |  |  | ADW15000 | Q6115.9 | 77 | 0 |
|  |  |  |  |  | Q6115.22 | 77 | 0 |
|  |  |  |  |  | Q6115.16 | 77 | 0 |

- These Samples were subjected to preconditioning (per J-STD-020 Level 3) prior to the start of the stress test. Level 3 preconditioning consists of the following:

- Bake: 24 hrs @ 125ºC,

- Soak: Unbiased Soak: 192 hrs @ 30ºC, 60%RH,

- Reflow: 3 passes through an oven with a peak temperature of 260ºC.

Samples of the many devices manufactured with these package and process technologies are continuously undergoing reliability evaluation as part of the ADI Reliability Monitor Program.  Additional qualification data is available on Analog Devices' web site.

ESD Test Results

The results of Human Body Model (HBM), Machine Model (MM), and Field Induced Charge Device Model (FICDM) ESD testing are summarized in the ESD Results Table.  ADI measures ESD results using stringent test procedures based on the specifications listed.  Any comparison with another supplier's results should ensure that the same ESD test procedures have been used.  For further details, please see the EOS/ESD chapter of the ADI Reliability Handbook (available via the 'Quality and Reliability' link at the Analog Devices Website (Analog Website).

Table 4: ESD Test Results

| ESD Model | Package | ESD Test Spec | RC Network | Highest Pass Level | First Fail Level | Class |
| --- | --- | --- | --- | --- | --- | --- |
| FICDM | 72-LFCSP | JESD22-C101 | 1Ω, Cpkg | ±1000V | ±1500V | C5 |
| HBM | 72-LFCSP | ANSI/ESD STM5.1-2007 | 1.5kΩ, 100pF | ±2000V | NA | 2 |
| MM | 72-LFCSP | ANSI/ESD STM5.2-1999 | 0Ω, 200pF | ±100V | ±200V | M2 |

Latch-Up Test Results

Six samples of the AD9122 were Latch-up tested at Ta=25ºC per JEDEC Standard JESD78, Class I, Level A.  All six devices passed.

Approvals

Reliability Engineer: Lejun Hu

This report has been approved by electronic means (4.0).

Additional Information

Data sheets and other additional information are available on Analog Devices' web site.