| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3/77 | Pass |
| Electrostatic Discharge Machine Model | ESD Association STM5.2-1999 |  | Pass ±200V |
| Electrostatic Discharge Human Body Model | ESD Association STM5.1-2007 |  | Pass ±2000V |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 |  | Pass ±1500V |