ADI PCN 11_0091

| ADXL346 QUALIFICATION PLAN |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Expected Completion Date |
| Group D Sub-Group 4 | MIL-STD 883 M5005 | 3x42 | PASS |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3x77 | PASS |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3x77 | PASS |
| Unbiased Highly Accelerated Stress Test (UHAST) * | JEDEC JESD22-A118 | 3x77 | PASS |
| High Temperature Storage (HTS) | JEDEC JESD22-A103 | 3x77 | PASS |
| 1.2m Drop | CAM0091 | 3x32 | PASS |

*Preconditioned per JEDEC/IPC J-STD-020