| QUALIFICATION #9681: ADXL345 TSMC MEMS Only New Process Qualification |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3x77 | PASS |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3x77 | PASS |
| Autoclave (AC)* | JEDEC JESD22-A102 | 3x77 | PASS |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 3x77 | PASS |
| Unbiased Highly Accelerated Stress Test (UHAST) * | JEDEC JESD22-A118 | 3x77 | PASS |
| Low Temperature Storage (LTS) | JEDEC JESD22-A119 | 5x77 | PASS |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 5x77 | PASS |
| Mechanical Shock Powered | IEC 68 Part 2-27 Testgroup Ea | 3x10 | PASS |
| Random Drop | CAM0091 | 3x35 | PASS |

*Preconditioned per JEDEC/IPC J-STD-020