ADuM125xW Die Rev C – Automotive Grade 1 Qualification

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 3x77 6x45 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3x77 9x45 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 6x77 4x45 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 4x77 4x45 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 3x45 2x77 | Pass |
| Latch-Up | JEDEC Standard 78 | 6 | Pass |
| Electrostatic Discharge Human Body Model | ESD Association JEDEC JS-001-2011 | 3/voltage | Pass +/- 4000V |
| Electrostatic Discharge Machine Model | ESD Association JESD22-A115 | 3/voltage | Pass +/- 200V |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association JESD22-C101 | 3/voltage | Pass +/- 1250V1 |

*Preconditioned per JEDEC/IPC J-STD-020

1-All pins were zapped