AD8203 Die Revision C – Automotive Grade 1 Qualification

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 6x77 2x45 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 6x77 | Pass |
| Temperature Cycle (TC)*A | JEDEC JESD22-A104 | 7x77 2x45 1x32 | Pass |
| Temperature Cycle (TC)*B | JEDEC JESD22-A104 | 10x77 | Pass |
| Autoclave (AC)*A | JEDEC JESD22-A102 | 8x77 2x45 | Pass |
| Autoclave (AC)*B | JEDEC JESD22-A102 | 10x77 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 6x77 | Pass |
| Latch-Up | JEDEC Standard 78 | 1x6 | Pass |
| Electrostatic Discharge Human Body Model | ESD Association JEDEC JS-001-2011 | 1x24 | Pass +/- 2000V |
| Electrostatic Discharge Machine Model | ESD Association JESD22-A115 | 1x6 | Pass +/- 100V |
| Electrostatic Discharge Field-Induced Charged Device ModelA | ESD Association JESD22-C101 | 1x18 | Pass +/- 1250V1 |
| Electrostatic Discharge Field-Induced Charged Device ModelB | ESD Association JESD22-C101 | 1x18 | Pass +/- 1250V1 |
| Temperature Humidity Bias (THB) | JESD22-A101 | 3x77 | Pass |

*Preconditioned per JEDEC/IPC J-STD-020

1-All pins were zapped

A-Tests were completed on 8-mSOIC

B-Tests were completed on 8-SOIC_N