**PCN12\_0239**

|  |
| --- |
| QUALIFICATION RESULTS |
| Test | Conditions | Sample Size | Results |
| Temperature Cycle (TC)\* | **JEDEC** *JESD22-A104* | **8x77** | **Pass** |
| Autoclave (AC)\* | **JEDEC** *JESD22-A102* | **8x77** | **Pass** |
| High Temperature Storage Life (HTSL) | **JEDEC** *JESD22-A103* | **3x77** | **Pass** |
| Solder Heat Resistance (SHR) | **ADI-0049** | **7x15****1x30** | **Pass** |

\*Preconditioned per JEDEC/IPC J-STD-020