Qualification Results for AD623 with 2XBUFF

| QUALIFICATION RESULTS |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| High Temperature Operating Life (HTOL)* | JEDEC JESD22-A108 | 9 x 77 | Pass |
| Highly Accelerated Stress Test (HAST)* | JEDEC JESD22-A110 | 3 x 77 4 x 45 | Pass |
| Temperature Cycle (TC)* | JEDEC JESD22-A104 | 9 x 77 | Pass |
| Temperature/Humidity/Bias (THB)* | JEDEC JESD22-A101 | 3 x 77 1 x 30 | Pass |
| Autoclave (AC)* | JEDEC JESD22-A102 | 9 x 77 | Pass |
| High Temperature Storage Life (HTSL) | JEDEC JESD22-A103 | 9 x 77 | Pass |
| SHR (Solder Heat Resistance)* | ADI-0049 | 1 x 30 | Pass |
| Latch-Up | JEDEC Standard 78 | 1 x 6 | Pass |
| Electrostatic Discharge Human Body Model | ESD Association STM5.1-2007 | 1 x 18 | Pass ±3500V |
| Electrostatic Discharge Field-Induced Charged Device Model | ESD Association STM5.3.1-1999 | 1 x 18 | Pass ±1250V |

*Preconditioned per JEDEC/IPC J-STD-020