| PCN 13_0321 Qualification Summary |  |  |  |
| --- | --- | --- | --- |
| Test | Conditions | Sample Size | Results |
| Temperature Cycle Condition ‘C’ (TC)* | JEDEC JESD22-A104 | 3x77 | PASS |
| Unbiased Highly Accelerated Stress Test (UHAST)* | JEDEC JESD22-A118 | 3x77 | PASS |

*Preconditioned per JEDEC/IPC J-STD-020 MSL3